## Slide 1: Photo-assisted Flow Battery Charging
Wes Fermanich
B.S.E. Materials Science and Engineering (Honors Capstone)
Minor in Energy Science and Policy
Advisor: Prof. David Kwabi
Department of Mechanical Engineering

## Slide 2: Background
Problem
Intermittency of solar energy requires coupling with energy storage systems
Coupling these systems causes efficiency loses and takes up greater space
Solution
Integration of dye-sensitized solar cells (DSSCs) with redox flow batteries  solar flow batteries
Direct storage of solar-generated energy in battery, aiding the charging process
Li, W., & Jin, S. (2020). Design Principles and Developments of Integrated Solar Flow Batteries. Accounts of Chemical Research, 53(11), 2611-2621. doi:10.1021/acs.accounts.0c00373
Solar flow battery schematic

## Slide 3: Work Completed
Photoanode Production
Paste formulation  paste dispersion  drying  dye-sensitization
Photoanode Testing
Cyclic voltammetry: apply voltages to photoanode in electrolyte and measure current response
Sensitized samples for different amounts of time
Uncoated
Coated & dried
Sensitized

## Slide 4: Photoanode Testing Set Up
~72 hrs
5 hrs
20 hrs
13 hrs
0 hrs
All anodes had an active area of roughly 2.5 cm2 apart from S2 which had an active area of ~3.1 cm2
Photoanode
Gasket
Electrolyte w/ stir bar
counter electrode

## Slide 5: Testing Results
Sample | Sensitization Time (hrs) | Max Power (mW)
R1 | 5 | 0.176
R2 | 20 | 0.226
R3 | 13 | 0.126
S2 | ~72 | 0.366
S2 norm | ~72 | 0.305
Chart: Potential vs. Porous Carbon (mV)

## Slide 6: SEM Images
Heat treated and unsensitized
Air-dried, not heat treated

## Slide 7: Looking Forward
Photoanode Production
Finalize paste formulation and dispersion
Determine parameters of interest for performance
Implement into Flow Cell
Test for full charging cycle under illumination
Test with other electrolytes
Photoanode Characterization
Surface structure analysis
Electrical performance testing

## Slide 8: Acknowledgments
Professor David Kwabi
Sanat Modak
Cansu Doganay
Professor Zetian Mi
Yixin (Arthur) Xiao
Dr. Pilar Herrera-Fierro
CoE Engineering Honors Staff

## Slide 9: Additional Slides

## Slide 10
Photoanode Performance Theory
FTO
TiO2
Z-907 dye

## Slide 11
Z-907 Dye Structure & Properties
Z-907 dye
HOMO: -5.4 eV
LUMO: -3.8 eV
Effective “band gap”: ~1.6 eV
775 nm
**hydrophobic
https://www.sciencedirect.com/topics/engineering/solar-spectrum

## Slide 12: I-V Curves
Sample | Sensitization Time (hrs) | Open Circuit Voltage (mV) | Short Circuit Current (mA)
R1 | 5 | 243 | 1.83
R2 | 20 | 213 | 2.62
R3 | 13 | 210 | 1.56
S2 | ~72 | 304 | 3.99
S2 norm | ~72 | 304 | 3.32
Chart: Potential vs. Porous Carbon (mV)

## Slide 13: Total Photoanode Testing Results
Sample | Sensitization Time (hrs) | Open Circuit Voltage (mV) | Short Circuit Current (mA) | Max Theoretical Power (mW) | Max Power (mW) | Fill Factor | Series Resistance (Ω)
R1 | 5 | 243 | 1.83 | 0.445 | 0.176 | 39.6% | 32.4
R2 | 20 | 213 | 2.62 | 0.558 | 0.226 | 40.5% | 29.0
R3 | 13 | 210 | 1.56 | 0.328 | 0.126 | 38.5% | 35.8
S2 | ~72 | 304 | 3.99 | 1.21 | 0.366 | 30.2% | 47.4
S2 norm | ~72 | 304 | 3.32 | 1.01 | 0.305 | 30.2% | -