## Slide 1
Background
Heterogeneous inner-sphere transition metal-ion charge transfer (CT) reactions involve the formation of a chemical bond between the electrode and the metal ion
They are relevant for electroplating, chemical sensors, corrosion prevention, and redox flow batteries (RFBs) for grid-scale clean energy storage
Widespread commercialization of vanadium RFBs (Figure 1) is limited by slow V2+/V3+ CT kinetics and low energy efficiency
Simple descriptors for inner-sphere CT kinetics could enable rational design of more active electrocatalysts
References
Introduction
Explaining Kinetic Trends of Inner-sphere Transition Metal Ion Redox Reactions at Electrodes
Harsh Agarwal, Jacob Florian, Daniel Pert (Honors Capstone), Bryan R. Goldsmith, Nirala Singh
Kinetics of other heterogenous CT reactions from literature involving transition metal ion redox couples also correlate with d-band center (Figure 10)
Acknowledgements
This research used the resources of the National Energy Research Scientific Computing Center (NERSC), a U.S. Department of Energy Office of Science User Facility operated under Contract No. DE-AC02-05CH11231 using NERSC award BES-ERCAP0022175
We hypothesize that the d-band center of the electrode affects the adsorption energy of the CT intermediate and therefore acts as a descriptor for heterogenous inner-sphere CT kinetics
The adsorption energy of the proposed intermediate *[X─MX5] depends on overlap between the d-orbital of the electrode and the p-orbital of the ligand X according to d-band theory (Figure 11)
A lower d-band center results in greater occupancy in the anti-bonding orbitals, leading to weaker adsorption; conversely, a higher d-band center leads to stronger adsorption
Figure 11. (a) Free energy profile for inner-sphere heterogeneous metal ion CT reaction (b) Reaction steps involving transition metals M1 and M2 and neutral ligand X. εX is the electronic energy of the p-orbital of ligand X, and εF is the electrode Fermi level
Results (cont.)
Use Tafel method (Figure 3) to find exchange current density and apparent activation energy of V2+/V3+ reaction on different electrodes as a function of the state of charge (SoC)
Develop a microkinetic model to determine the RDS for V2+/V3+ based on kinetic measurements
Use DFT calculations to evaluate adsorption energy of *[O─V(H2O)4SO4] intermediate on metals to with varying d-band center (Figure 4,5) to see if correlation exists
Extract kinetic data from literature for other heterogeneous metal-ion CT reactions to test validity of d-band center as kinetic descriptor
Previous work using extended X-ray absorption fine structure (EXAFS) spectroscopy has confirmed the structure of V2+ and V3+ in perchloric, hydrochloric, and sulfuric acid (Figure 2) [2,3]
V2+/V3+ CT kinetics on glassy carbon are determined by the energy of the adsorbed intermediate
Based on kinetic measurements, we hypothesize the *[O─V(H2O)4SO4] intermediate occurs on metal surfaces in H2SO4, and that the same effect of adsorption energy on CT kinetics holds [4]
The average energy of the d electrons (d-band center) may act as a descriptor for CT kinetics
[1] Upgrading the Vanadium Redox Battery, Pacific Northwest National Laboratory.
[2] H. Agarwal, J. Florian, B.R. Goldsmith, N. Singh, ACS Energy Lett. 4 (2019) 2368–2377.
[3] H. Agarwal, J. Florian, B.R. Goldsmith, N. Singh, Cell Rep. Phys. Sci. 2 (2021) 100307.
[4] J. Florian, H. Agarwal, N. Singh, B. R. Goldsmith, Chem. Sci., 12 (2021) 12704–12710.
[5] Pérez-Jiménez, A. I.; Lyu, D.; Lu, Z.; Liu, G.; Ren, B. Chem. Sci., 11 (2020), 4563–4577.
[6] F. Musiani, A. Giorgetti, Int’l Rev. of Cell and Molecular Biology, (2017), 49–77.
[7] H. Agarwal, J. Florian, D. Pert, B.R. Goldsmith, N. Singh, ACS Catal. (2023) 2223–2233.
Results
∝
Figure 8. Computed free energy profile of adsorbed vanadium intermediate on metals that are (a) experimentally tested, i.e., Bi, Au, Ag, Cu, and W and (b) not experimentally tested, i.e., Rh, Fe, Cr, and Ta for V2+/V3+ kinetics (c) Exchange current density as a function of calculated adsorption energies of *[O─V(H2O)4SO4] on Au, Ag, Cu, Bi, and W electrodes for V2+/V3+ reaction
Kinetic measurements (Figure 6), microkinetic modelling (Figure 7), and adsorption energy calculations (Figures 8,9) all indicate an inner-sphere mechanism for V2+/V3+ on metal electrodes
Results indicate CT is the rate-determining step and *[O─V(H2O)4SO4] is the adsorbed intermediate
Figure 9. Adsorption energy of *[O─V(H2O)4SO4] calculated with (a) metadynamics simulations with explicit solvent and (b) static gas-phase calculations shown against the d-band center
Conclusions
(b)
(a)
(c)
Figure 1. A VFRB converts V3+ to V2+ during charging and V2+ back to V3+ during discharging [1]
+
V
H2O
H2O
H2O
H2O
H2O
SO4
3+
V
H2O
H2O
H2O
H2O
H2O
H2O
2+
V
H2O
H2O
H2O
H2O
H2O
Cl
(a)
(b)
(c)
(d)
Figure 2. Structure of V3+ complex in the presence of (a) perchloric, (b) hydrochloric, and (c) sulfuric acid. Note that an additional chloride may complex with V3+ in hydrochloric acid (d) The adsorption energy of the bridged intermediate controls CT kinetics on a glassy carbon electrode
Methods
Figure 3. Logarithm of kinetic current density vs. overvoltage (Tafel plot) used obtain exchange current density ()
Figure 4. Metadynamics can be described as filling the valleys of the free energy landscape with computational sand. Gaussian “hills” are deposited to bias the system away from values of the collective variable that have been sampled. Image reprinted from ref. 6
Figure 6. (a) Exchange current densities () from the Tafel method (b) apparent activation energies (), and (c) apparent frequency factors as a function of SoC for V2+/V3+ reaction on Au, Ag, Cu, Bi, W, edge plane pyrolytic graphite (EPPG), and glassy carbon (GC) electrodes
∝
Chart: State of Charge / %
Chart: State of Charge / %
Chart: State of Charge / %
Figure 7. Predicted trends of (a) exchange current density, (b) apparent activation energy, and (c) apparent frequency factor with SoC assuming electron transfer is the rate determining step
(b)
(a)
Figure 10. Correlation between d-band center and kinetics of different inner-sphere redox couples: (a) V2+/V3+ in H2SO4, (b) Cr2+/Cr3+ in NaClO4, (c) Co2+/Co3+ in NaClO4 + HClO4, and (d) Fe2+/Fe3+ in K2SO4 + H2SO4 (b-d taken from the literature)
Chart: State of Charge / %
| 100 | 80 | 50 | 30 | 10
Ag disk_Tafel | 0.68973 | 0.62508 | 0.67273 | 0.64846 | 0.41318
Au film_Tafel | 0.96693 | 0.63057 | 0.41536 | 0.27107 | 0.12005
Cu disk_Tafel | 0.53231 | 0.62102 | 0.73826 | 0.70706 | 0.52384
Bi disk_Tafel | 0.065194 | 0.10985 | 0.12907 | 0.10977 | 0.048391
EPPG_Tafel | 0.004949 | 0.012081 | 0.013699 | 0.012618 | 0.0089209
GC_Tafel | 0.0051452 | 0.0038574 | 0.0028913 | 0.001488 | 0.0013502
W disk_Tafel | 1.3554 | 3.9278 | 4.7823 | 4.3145 | 2.215
Chart: State of Charge / %
| 100 | 80 | 50 | 30 | 10
Au (Tafel) | 19.9278 | 21.1009 | 26.0602 | 26.9282 | 30.4409
GC (Tafel) | 35.0418 | 36.5891 | 44.5456 | 53.8864 | 68.5365
Ag (Tafel) | 22.1169 | 24.4182 | 25.2421 | 23.65 | 25.746
Cu (Tafel) | 20.0151 | 27.8752 | 31.2939 | 32.0297 | 40.8583
Bi (Tafel) | 6.6289 | 18.4878 | 18.0073 | 20.3344 | 28.2443
EPPG_Tafel | 44.3494 | 24.6976 | 24.9836 | 25.81 | 30.6679
W_Tafel | 20.4308 | 15.6353 | 8.763 | 13.6907 | 24.5479
(a)
(b)
(c)
Chart: State of Charge / %
| 100 | 80 | 50 | 30 | 10
Au_Tafel | 3067.1375 | 3292.8213 | 17802.6037 | 14256.953 | 29732.6189
Ag_Tafel | 5537.5088 | 13315.7124 | 17907.9495 | 9392.812 | 14391.6003
Cu_Tafel | 1838.6741 | 54014.0783 | 259367.1748 | 328404.0536 | 8948531.5127
GC_tafel | 7115.281 | 9996.5969 | 179871.8623 | 4876800.8533 | 1193313824.055
Bi_Tafel | 0.95628 | 202.0267 | 187.8042 | 435.5894 | 4467.1236
EPPG_Tafel | 206695.0918 | 292.0427 | 367.8223 | 463.0338 | 2340.2195
W_tafel | 5118.9264 | 2100.8557 | 164.7452 | 1070.1991 | 43608.1788
0.1
10
103
105
107
109
(a)
(b)
(c)
(d)
(a)
(b)
Higher d-band center leads to stronger binding, as expected from d-band theory
Same trends in both aqueous phase and gas phase, but stronger correlation in aqueous phase
We demonstrate for the first time that the d-band electronic structure of the electrode is related to the heterogeneous inner-sphere CT kinetics of transition metal ions [7]
We focus on the V2+/V3+ reaction because the mechanism is not well understood despite its importance in commercialized vanadium-based redox flow batteries for energy storage
W is the most active electrocatalyst reported for the V2+/V3+ reaction to-date
Our findings extend the applicability of the d-band model, which is ubiquitously used in heterogeneous catalysis, to transition metal ion adsorbates for charge transfer reactions
Identification of d-band center as kinetic descriptor will enable rational design of alloys or core-shell catalysts with a desired d-band center to maximize inner-sphere CT kinetics
Figure 5. Simulation cell used to evaluate adsorption energy of *[O─V(H2O)4SO4] on Au(111) using metadynamics (a) before desorption and (b) after desorption
(a)
(b)
(c)
(a)
(b)